## Slide 1
EARTHMOVER WHEELS & SAFETY
Titan® doesn’t just follow safety standards, we redefine them
This document is proprietary and confidential. No part of this document may be disclosed in any manner to a third party without the prior written consent of the Titan engineering and legal department.

## Slide 2
Earthmover Wheels & Safety
Contents
Types / Construction / Manufacturing
Inspections:
  How-to
  Field Inspections
  Best Practices
This document is proprietary and confidential. No part of this document may be disclosed in any manner to a third party without the prior written consent of the Titan engineering and legal department.

## Slide 3
Titan International
Wheel Footprint / History
Latin / South America | 
 | Atibaia, Brazil
 | Buenos Aires, Argentina
 | Cali, Columbia
 | Iquique, Chile
/ | Lima, Peru
 | Parauapebas, Pará, Brazil
 | São Paulo, Brazil
/ | Santiago, Chile
Australia | 
 | Emerald, QLD
 | Mildura, VIC
 | Muswellbrook, NSW
/ | Perth, WA
 | Sydney, NSW
/ | Yatala, QLD
Asia / Africa | 
 | Aydin, Turkey
 | Heidelberg, South Africa
 | Jakarta, Indonesia
 | Liuzhou, China
 | Tianjin, China
 | Visakhapatnam, Andhra Pradesh, India
 | Tires
 | Wheels
 | Undercarriage
 | Mining Services
 | Distribution
Europe / Russia |  |  | 
 | Ceprano, Italy |  | Kidderminster, UK
 | Fanano, Italy |  | Monreal del Campo, Spain
 | Finale Emilia, Italy |  | Potenza, Italy
 | Flers, France |  | St. Helens, UK
 | Gevelsberg, Germany |  | Valsamoggia, Italy
 | Jesi, Italy |  | Volgograd, Russia
North America | 
 | Quincy, IL (International headquarters)
 | Bryan, OH
 | Des Moines, IA
 | Elkhorn, WI
 | Freeport, IL
 | Fort McMurray, AB, Canada
 | Gillette, WY
 | Holden, WV
 | Jefferson, GA
 | Querétaro, Mexico
 | Saskatoon, SK, Canada
 | Union City, TN
 | West-Chicago, IL
 | Winston-Salem, NC
+
=
+
STEEL PRODUCTS DIVISION
[
]

## Slide 4
Wheel Types (Industry Common)
Single, 3-Piece & 5-Piece Wheels
Single-piece >>
Single Piece roll-formed rim contour
Formed and press-fit disc for structural integrity and minimized weight
Fully e-coated for corrosion protection and superior finish
3-piece >>
Typically for small wheel loader, grader and harvester applications
Removable side-ring and lock-ring for ease of tire mounting and servicing
Square face lock-ring to prevent incorrect installation
5-piece >>
Removable side flanges, bead-seat, and lock-ring for ease of tire servicing
Square face lock-ring to prevent incorrect installation
HSLA (High Strength Low Alloy) materials used to maximize fatigue life
Forged/Seamless flanges available (optional on some sizes)
Integral continuous pry bar slot on 33” and above for ease of component servicing
This document is proprietary and confidential. No part of this document may be disclosed in any manner to a third party without the prior written consent of the Titan engineering and legal department.

## Slide 5
Wheel Types (Industrial 10 bar Wheels)
Standard vs. Industrial
10 bar (Industrial)
  Designed for 145 psi (10 bar) cold pressures
Standard (Earthmover)
  Not designed for hot pressures above 145 psi
  EH rims may not be used to create 10 bar wheels
This document is proprietary and confidential. No part of this document may be disclosed in any manner to a third party without the prior written consent of the Titan engineering and legal department.

## Slide 6: Wheel Construction (Standard)
Rim Base Components
This document is proprietary and confidential. No part of this document may be disclosed in any manner to a third party without the prior written consent of the Titan engineering and legal department.

## Slide 7
Wheel Construction (Industrial 10 bar Wheels)
This document is proprietary and confidential. No part of this document may be disclosed in any manner to a third party without the prior written consent of the Titan engineering and legal department.

## Slide 8
Wheel Manufacturing
Product Quality Assurance
Each component we produce
meets the highest quality standards
possible, beginning with CNC
precision machining
By using state-of-the-art welders and
camera monitoring, we get 100 percent
penetration on each weld to meet
AWS standards. All wheels are
serialized for traceability.
Each component is verified using
coordinate measuring machines.
Titan welds to AWS standards
and uses state-of-the-art x-ray
technology to verify 100% weld
integrity.
Critical surfaces are shot peened to
extend wheel life.
Titan-manufactured loose components
are fully coated with durable powder
paint to ensure long product life.
This document is proprietary and confidential. No part of this document may be disclosed in any manner to a third party without the prior written consent of the Titan engineering and legal department.

## Slide 9
Wheel Manufacturing
Non-Destructive X-Ray Capabilities
This document is proprietary and confidential. No part of this document may be disclosed in any manner to a third party without the prior written consent of the Titan engineering and legal department.

## Slide 10
Common Field Issues
Causes of premature FAILURE or worse, a life-threatening accident:
  Age
  Overload
  Poorly maintained haul roads
  Poor operating conditions
  Misuse of equipment
  Under inflated tires
Washed out lock ring grooves stress fatigue fractures caused by:
  Friction welding
  Aggregate
  Corrosion
Great reasons for doing a safety inspection of the rim
Wheel Inspections (How-to)
This document is proprietary and confidential. No part of this document may be disclosed in any manner to a third party without the prior written consent of the Titan engineering and legal department.

## Slide 11
Components
Identification:
Part Number
Serial Number
Size
“Gutter section”
“Back section”
Stud holes
Bolting plate weld
Rim base welds
This document is proprietary and confidential. No part of this document may be disclosed in any manner to a third party without the prior written consent of the Titan engineering and legal department.
Wheel Inspections (How-to)

## Slide 12
Hardware is considered as consumable product.
Hardware includes:
  Bead Seat Bands
  Rim Flanges
  Locking Rings
Hardware that is suspected of having defects or distortion, shall be discarded.
All hardware shall be inspected by Field and Tire Shop Personnel prior to it’s reuse.
OSHA 29 CFR 1910
Components:
Points to Consider
This document is proprietary and confidential. No part of this document may be disclosed in any manner to a third party without the prior written consent of the Titan engineering and legal department.
Wheel Inspections (How-to)

## Slide 13
Components:
Common Damage Areas
This document is proprietary and confidential. No part of this document may be disclosed in any manner to a third party without the prior written consent of the Titan engineering and legal department.
Wheel Inspections (How-to)

## Slide 14
Fill Media Types
Standard:
Air
Nitrogen
Tire Life® (supplemental protectant)
Alternate:
Liquid Ballast (Water, Foam, Poly) – cost, maint, no checks
Foam Core (Trojan™ Liner) – cost, maint.
Non-Pneumatic, Solid Tires – ride
This document is proprietary and confidential. No part of this document may be disclosed in any manner to a third party without the prior written consent of the Titan engineering and legal department.
Wheel Inspections (How-to)

## Slide 15
Inflation Pressure Range by tire type
This document is proprietary and confidential. No part of this document may be disclosed in any manner to a third party without the prior written consent of the Titan engineering and legal department.
Fill Media Types:
Inflation Pressure Ranges
Wheel Inspections (How-to)

## Slide 16
Condition:
  Welded Wheel / Welding on Mounted Wheel
Cause:
  Gases may be present within the tire cavity and heat form welding will cause a drastic rise in pressure, this can result in a rapid air loss
Best Practice:
  Never attempt to weld on a deflated tire and rim assembly
  Never attempt to weld on an inflated tire and rim assembly
This document is proprietary and confidential. No part of this document may be disclosed in any manner to a third party without the prior written consent of the Titan engineering and legal department.
Inspections (Field)
Mounting / Inflating

## Slide 17
Rim Base / Gutter
Pressure
Zone
Non-Pressure
Zone!!
  Danger Zone:
Inspections (Field)
This document is proprietary and confidential. No part of this document may be disclosed in any manner to a third party without the prior written consent of the Titan engineering and legal department.

## Slide 18
  Condition:
    Cracking
    Corrosion
  Cause:
    Overload / Under-Inflation
    Age
  Best Practice Action:
    Recommended service life is 10,000 operating hours
    Wheels should be sand blasted and inspected for fatigue and hairline cracks
    At minimum, rim base, spud, and valve hardware should be changed every other tire change
    Use Tire Life®
This document is proprietary and confidential. No part of this document may be disclosed in any manner to a third party without the prior written consent of the Titan engineering and legal department.
Inspections (Field)
Rim Base / Gutter

## Slide 19
Profile Gauge
(“Go, No-Go” Gauge)
O-Ring Groove
O-Ring / Wheel Interface
ID of Rim, houses the Disc, and seats the components
Lock ring grooves are inspected using a gauge for wear & damage
Lock Ring Groove
This document is proprietary and confidential. No part of this document may be disclosed in any manner to a third party without the prior written consent of the Titan engineering and legal department.
Inspections (Field)
Rim Base / Gutter

## Slide 20
Condition:
  Air Loss / Exposed O-Ring
Cause:
  Flattened O-Ring (age, under-inflation: shifting components)
  Rolled O-Ring (misalignment during mounting)
Best Practice Action:
  De-mount, check for burrs, replace O-Ring, re-mount with proper inflation pressure, check in 24 hours
  Replace at every tire change
Flattened O-Ring
Rolled O-Ring
This document is proprietary and confidential. No part of this document may be disclosed in any manner to a third party without the prior written consent of the Titan engineering and legal department.
Inspections (Field)
O-Rings

## Slide 21
Sprung Lock-Ring
Condition:
  Wear
  Corrosion
Cause:
  Under-inflated tire rocking on the wheel
  Age and/or storage
Best Practice Action:
  Replace
This document is proprietary and confidential. No part of this document may be disclosed in any manner to a third party without the prior written consent of the Titan engineering and legal department.
Inspections (Field)
Bead Seat Band

## Slide 22
Condition:
  Bent / Deformed
  Extreme Wear
Cause:
  Mounting Damage
  Old stock, over-deflection of tire
Best Practice Action:
  Replace
This document is proprietary and confidential. No part of this document may be disclosed in any manner to a third party without the prior written consent of the Titan engineering and legal department.
Inspections (Field)
Flange

## Slide 23
(Main Retainer for the rim components)
Condition:
  Stretched / Worn / Sprung
  Cracked
  Corrosion
Cause:
  Age and/or storage
Best Practice Action:
  Visually inspect for wear, “sprung”, stretched, corrosion, cracks, flat spots, misalignment and warping
  The Lock Ring needs to be replaced when the two ends no longer touch when loose
BAD (sprung, rusted)
GOOD
CRACKED
BAD (sprung)
This document is proprietary and confidential. No part of this document may be disclosed in any manner to a third party without the prior written consent of the Titan engineering and legal department.
Lock Rings
Inspections (Field)

## Slide 24
(Driver keys help to prevent premature metal to metal wear by keeping rim components in place and keeps debris out (more pressure on O-ring in high torque / static turning scenarios))
Condition:
  Missing Key
  Cracked Pocket
  Misaligned/Indexed Components
Cause:
  Damage, Age, Missed
Best Practice Action:
  Install new Driver Key
  Wheel needs replaced (pocket)
  OSHA 29 CFR 1910
Missing Driver Key; Indexed components
OSHA 29 CFR 1910 Violation
Cracked Driver Pocket
This document is proprietary and confidential. No part of this document may be disclosed in any manner to a third party without the prior written consent of the Titan engineering and legal department.
Driver Key / Pocket
Inspections (Field)

## Slide 25
What questions do you have?
Pete Kearney
Global Director of Mining Tires & Wheels
(515) 710-7724
Willie Yeber
OTR Tire & Wheel Specialist & Territory Sales Manager (305) 496-2516
Matt Miller
Director of Engineering, R&D (OTR)
Matt Werstein
Engineering Manager R&D / Product Manager (OTR)
Thank you!
This document is proprietary and confidential. No part of this document may be disclosed in any manner to a third party without the prior written consent of the Titan engineering and legal department.