## Slide 1: Experimental and Numerical Analyses of Leachate from Air Cooled Blast Furnace Slag Materials
Ali Arda CAKALOGLU – Graduate Research Assistant
Dr. Angela FARINA - Postdoctoral Research Associate
Dr. Bora CETIN - Principal investigator
2025 National Slag Association Annual Meeting
Ritz-Carlton Naples, Tiburon, Florida
September 15-18, 2025

## Slide 2: INTRODUCTION
SLAG AS A CONSTRUCTION MATERIAL
‘Appian Way’ in Italy (312 BC)
Modern Road Application

## Slide 3: INTRODUCTION
Blast furnace slag production process.(Pasetto et al., 2023)
Steel slag production and disposal routes (Song et al., 2021)
16 million tons produced annually
54% Blast furnace slag
(USGS, 2023)
SLAG PRODUCTION

## Slide 4: GOAL OF THE PROJECT
Develop a new test method to evaluate whether ACBFS are properly tested from the environmental perspective before their use in construction applications
Comparing different leaching tests
Determine the behavior of leaching
Evaluate potential remediation
Industrial co-product of the iron & steel industry
Behavior varies by slag type & test method
MAIN GOAL
AIR-COOLED BLAST FURNACE SLAGS (ACBFS)

## Slide 5
MATERIALS
Gary Works Indiana
Holcim
Pennsylvania
Burns Harbor Indiana
(Treated)
Harbor West
Indiana
(Untreated)
ACBFS
Gradation Distribution of ACBFS Materials
Index and Compaction Properties of ACBFS:
( U : Untreated, T : Treated )

## Slide 6
MATERIALS
SUBGRADE SOILS
Gradation Distribution of Soil Materials
Silt
Sand
Clay
Index and Compaction Properties of Soils:

## Slide 7
METHODS
pH, Electrical conductivity, Oxidation reduction potential, Alkalinity, Sulfate and Sulfur content, Color, Odor (H₂S), Metals concentration
LEACHING TESTING
ITM-212 Protocol
(ACBFS only - 1, 3, 7, 15 days)
Stagnant Sequential Batch
(ACBFS and subgrade soil - 1, 7, 30, 90, 180 days)
Sequential Column Test
(ACBFS and subgrade soil)
Stockpile Large Boxes

## Slide 8
ITM-212 Protocol
SEQUENTIAL BATCH TEST
L/S of 0.4 mL/g-dry
1, 3, 7, and 15 days
L/S of 10 mL/g-dry
1, 7, 30, 90, 180 days
METHODS
Deionized water

## Slide 9
SEQUENTIAL COLUMN LEACHING TEST
ACBFS
Subgrade
Peristaltic Pump (30 ml/h)
METHODS

## Slide 10
STOCKPILES
Harbor West (U) ACBFS
Burns Harbor (T) ACBFS
Holcim ACBFS
Gary Works ACBFS
METHODS
Geotextile
( U : Untreated, T : Treated )

## Slide 11
ITM-212
Stagnant Batch Test
Upper limit
Lower limit
Upper limit
Lower limit
RESULTS
The Upper and lower limits are imposed by ITM 212 protocol
( U : Untreated, T : Treated )

## Slide 12
ITM-212
Stagnant Batch Test
EPA limit
EPA limit
RESULTS
The 250 mg/L EPA thresholds are secondary drinking water regulations. They are not mandatory
EPA limit
EPA limit
( U : Untreated, T : Treated )

## Slide 13
RESULTS
SEQUENTIAL STAGNANT BATCH TEST
( U : Untreated, T : Treated )

## Slide 14
EPA limit
EPA limit
EPA limit
When used together with soils, ACBFS shows significantly reduced leachate sulfate concentrations due to soil buffering.
RESULTS
SEQUENTIAL STAGNANT BATCH TEST
( U : Untreated, T : Treated )

## Slide 15
RESULTS
Upper limit
Lower limit
SEQUENTIAL COLUMN LEACHING TEST
EPA limit
( U : Untreated, T : Treated )

## Slide 16
RESULTS
STOCKPILES
Upper limit
The test started in February, and the results cover the period from February to September.
Lower limit
EPA limit
( U : Untreated, T : Treated )

## Slide 17
CONCLUSIONS
Results vary depending on the applied methodology
Interaction with different soils can mitigate potential environmental impacts
The treatment method provides less electrical conductivity, lower sulfate and sulfur concentrations
These observations highlight the potential value of developing a more representative testing approach rather than relying on a single standardized protocol.

## Slide 18
FUTURE WORKS
FATE AND TRANSPORT MODELLING
Numerical modeling is needed to serve as a bridge between laboratory experiments and real field conditions to achieve a better understanding of leachate behavior of the material.
HYDRUS1D
PHREEQC
HP1

## Slide 19
Acknowledgements
Dr. Bora Cetin – Michigan State University
Dr. Angela Farina - Michigan State University
Charles Ochola – National Slag Association
Kelly Cook - National Slag Association
Shawn Hahney - Phoenix Global
Paul Thomas – Holcim
Sean Marshall- Holcim
Francis Mark - Unites States Steel Corporation
Scott Flynn - Beemsterboer Companies (Gary Works)

## Slide 20
Thank you all for your kind attendence
Any Questions ?
cakalogl@msu.edu